

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |
| **SMILEY SQUEEGEE SPECIFICATION FOR FLEXO** | | | | |  |  |  |
|  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |
|  |  | |  | | --- | | PHOTO | |  |  |  |  |  |
| PRODUCT CODE | 7000-5MR20A60A |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |
| PROFILE | RECTANGULAR |  |  |  |  |  |  |
| THICKNESS | 5 MM. |  |  |  |  |  |  |
| DIMENSIONS WIDTH | 20 MM. |  |  |  |  |  |  |
| LENGTH PER ROLL | 183 CM. |  |  |  |  |  |  |
| HARDNESS | 60 ShA |  |  |  |  |  |  |
| MOLD | “A” |  |  |  |  |  |  |
| COLOUR | ORANGE |  |  |  |  |  |  |

|  |  |
| --- | --- |
| PRODUCT CODE | 7000-5MR20C75A |
|  |  |
| PROFILE | RECTANGULAR |
| THICKNESS | 5 MM. |
| DIMENSIONS WIDTH | 20 MM. |
| LENGTH PER ROLL | 183 CM. |
| HARDNESS | 75 ShA |
| MOLD | “C” |
| COLOUR | GREY |

